PART  1  GENERAL

1.1 	SECTION INCLUDES

A.	Lumonyx Polymer Panels.

1.2 	RELATED SECTIONS

A.	Section 08630 - Metal-Framed Skylights.

B.	Section 07900 - Joint Sealers.

C.	Section 08800 - Glazing

1.3 	REFERENCES

A.	ASTM Z 97.1 - American National Standard for Glazing Materials Used in Buildings -- Safety Performance Specifications and Methods of Test.

B.	ASTM D 256 - Standard Test Method for Determining the Pendulum Impact Resistance of Notched Specimens of Plastics.

C.	ASTM D 638 - Standard Test Method for Tensile Properties of Plastics.

D.	ASTM D 790 - Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials.

E.	ASTM D 792 - Standard Test Methods for Density and Specific Gravity (Relative Density) of Plastics by Displacement.

F.	ASTM D 1929 - Standard Test Method for Ignition Properties of Plastics.

G.	ASTM F 1233 - Standard Test Method for Security Glazing Materials and Systems.

1.4 	SUBMITTALS

A.	Submit under provisions of Section 01300.

B.	Product Data:  Manufacturer's data sheets on each product to be used, including:

1.	Physical properties including data on material weight, light transmission and thermal expansion.

Preparation instructions and recommendations

2.	Storage and handling requirements and recommendations.

3.	Installation methods and procedures, including edge engagement guidelines.

C.	Verification Samples:  Submit samples for each finish product specified, two samples, minimum size 2 inches by 3inches, representing actual product.

1.5 	DELIVERY, STORAGE, AND HANDLING

A.	Deliver Lumonyx Polymer sheets on enclosed pallets.

B.	Store products in manufacturer's unopened packaging until ready for installation.

C.	Store in dry, well-ventilated and covered areas at temperatures below 90 degrees F.

D.	Handle sheets carefully to prevent damage; do not drop, slide, or drag.

1.6 	PROJECT CONDITIONS

A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

1.7 	WARRANTY

A.	Provide Lumonyx Polymer sheets’ manufacturer's written warranty covering breakage.

PART  2  PRODUCTS

2.1 	MANUFACTURERS

A.	Provide products manufactured by Lumonyx, Inc.

4400 Oneal Street, Greenville, TX 75401 Tel (903) 454-0904 Fax (903) 454-3642

info@lumonyx.com 	www.lumonyx.com

B.	Substitutions are not allowed.

2.2 	LUMONYX POLYMER SHEET

A.	Lumonyx Polymer Sheet - General:  Comply with properties as follows:

1.	Specific gravity:  1.2, per ASTM D 792.

2.	Self ignition temperature:  1040 degrees F, per ASTM D 1929.

3.	Flash ignition temperature:  800 degrees F, per ASTM D 1929.

4.	Thickness: _______

5.	Color: _______

PART  3  EXECUTION

3.1 	EXAMINATION

A.	Inspect pallets upon delivery for evidence of damage.

B.	Inspect and verify that openings are correct size and conform to recommendations of the Lumonyx Polymer sheet manufacturer.

3.2 	PREPARATION

A.	Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

B.	Immediately prior to installation, expose glazing edges of plastic sheet by peeling back factory-applied protective masking to a dimension sufficient for edge engagement.

3.3 	INSTALLATION

A.	Install Lumonyx Polymer sheets in accordance with manufacturer's recommendations for edge engagement and expansion allowance.

B.	Employ only sealants and glazing accessories that have been approved by manufacturer of Lumonyx Polymer sheet.

C.	Remove protective masking immediately after all installation operations are completed.

3.4 	PROTECTION

A.	Protect installed products until completion of project.

B.	Affix polyethylene film or other covering approved by alabaster manufacturer to framing members, as required to protect plastic glazing from other construction operations.

C.	Repair or replace damaged products before Substantial Completion.

3.5 	SCHEDULE

END OF SECTION